## Slide 1: Technical Aspects of Bio-Fuels for Their Applications
Dr. L. C. Meher
Defence Institute of Bio-Energy Research (DRDO)
Project Site: Secunderabad

## Slide 2: Crude oil importing countries

## Slide 3: Crude oil import by India

## Slide 4: National Policy on Bio-Fuels (2008-09)
Target to blend 20% biofuel (Biodiesel/ Bioethanol) by 2017
Achieved 1.37% blending of ethanol with petrol
Capable to produce biodiesel140-300 million litre/year

## Slide 5: Genesis of biofuels
1st Generation Biofuels: from oilseed and crop sources, i.e. ethanol and biodiesel
2nd Generation Biofuels: agricultural waster and residues: lignocellulosic ethanol, green diesel, bio-butanol etc.
3rd Generation Biofuels: from algae
4th Generation Biofuels: Genetically modified plant derived fuels

## Slide 6: Bio-ethanol
Derived from sugarcane, sweet sorghum, sugar beet and cassava.
Developed standard IS 2796 (2008) for gasoline blended with 5% and 10% ethanol.

## Slide 7: Biodiesel as alternate to diesel
Biodiesel has the advantages over conventional diesel for
Low sulfur
No polyaromatics
High flash point
Excellent lubricity
Biodegradability
Quality achieved by complete transesterification of the triglyceride oil

## Slide 8: Biodiesel Quality Control
Biodiesel standard has been developed to ensure
Complete conversion of tiglyceride oil to fatty acid methyl esters (Biodiesel)
Biodiesel as fuel in compression ignition engines
IS 15607:2005 has been developed in Indian context which is Indian version of EN 12414 and ASTM D 6751

## Slide 9: Specification of biodiesel
IS 15607 in India for multiple non-edible oil feedstocks
EN 14214 in European countries (for biodiesel from rapeseed oil)
ASTM D 6751 in United States (for biodiesel derived from soybean oil)
The international biodiesel specification has the importance at the time of export of biodiesel to respective countries

## Slide 10: Properties of biodiesel
Sl. No. | Properties | IS 15607 | EN 14214 | ASTM D 6751
1. | Density @15oC, kg/m3 | 860-900 | 860-900 | n.s.
2. | Kinematic Viscosity at 40oC, cSt | 2.5-6.0 | 3.5-5.0 | 1.9-6.0
3. | Flash point, oC, min | 120 | 101 | 93
4. | Sulfur, ppm, max | 50 | 10 | 15
5. | Carbon Residue, % by mass, max | 0.05 | 0.3 | 0.05
6. | Sulfated Ash, % by mass, max | 0.02 | 0.02 | 0.02

## Slide 11: Properties of biodiesel
Density is achieved after the completion ot transesterification
Viscosity is achieved after transesterification, exception: castor oil based methyl esters
Viscosity range is low for EN 14214
Flash point is dependent upon the extent of removal of excess methanol used during biodiesel preparation
S content, sulfated ash and carbon residue depends upon the use of sulfuric acid, other alkali catalyst and the presence of impurities in the oil

## Slide 12: Properties of biodiesel
Sl. No. | Properties | IS 15607 | EN 14214 | ASTM D 6751
7. | Water content, ppm, max | 500 | 500 | 500
8. | Total contamination, ppm, max | 24 | 24 | n.s.
9. | Copper corrosion, 3h at 50oC, max | 1 | 1 | 3
10. | Cetane number, min | 51 | 51 | 47
11. | Acid Value, mgKOH/g, max | 0.5 | 0.5 | 0.5
12. | Methanol, % by mass, max | 0.2 | 0.2 | 0.2

## Slide 13: Properties of biodiesel
Water content: efficiency of water removal from biodiesel after washing
Total contaminants: solid impurity particles in biodiesel
Copper strip corrosion is easily achieved
Cetane number is achieved for biodiesel easily, specific to oils
Acid value of biodiesel dependent upon transesterification process, the value increases on storage
Methanol content is dependent upon efficiency of removal from biodiesel and affect the flash point

## Slide 14: Properties of biodiesel
Sl. No. | Properties | IS 15607 | EN 14214 | ASTM D 6751
13. | Ester content, % by mass, min | 96.5 | 96.5 | n.s.
14. | Linolenic acid methyl ester, % by mass, max | n.s. | 12 | n.s.
15. | Polyunsaturated (≥ 4 double bonds) methyl esters, % mass, max | n.s. | 1 | n.s.
16. | Monoglyceride, % by mass, max | n.s. | 0.8 | n.s.
17. | Diglyceride, % by mass, max | n.s. | 0.2 | n.s.
18. | Triglyceride, % by mass, max | n.s. | 0.2 | n.s.

## Slide 15: Properties of biodiesel
Ester content, glycerol and the glycerides are crucial parameter and achieved after complete conversion of oil to methyl esters.
Linolenic acid methyl ester and poly-unsaturated methyl esters are dependent upon the oil source, affect the oxidative stability of methyl esters

## Slide 16: Properties of biodiesel
Sl. No. | Properties | IS 15607 | EN 14214 | ASTM D 6751
19. | Free Glycerol, % by mass, max | 0.02 | 0.02 | 0.02
20. | Total Glycerol, % by mass, max | 0.25 | 0.25 | 0.24
21. | Phosphorus, ppm, max | 10 | 4 | 10
22. | Sodium and Potassium, ppm, max | To report | 5 | 5
23. | Calcium and Magnesium, ppm, max | To report | 5 | 5

## Slide 17: Properties of biodiesel
The limit of Na, K are specified so that the alkali used transesterification is efficiently removed during post-transeserification process.
P content is due to phospholipid present in the oil and also due to the use of phosphoric acid during degumming of oil.

## Slide 18: Properties of biodiesel
Sl. No. | Properties | IS 15607 | EN 14214 | ASTM D 6751
24. | Iodine Value, gI2/100g, max | To report | 120 | n.s.
25. | Oxidation Stability at 110oC, h, min | 6 | 6 | 3
26. | Cloud Point, oC | n.s. | n.s. | To report
27. | Distillation T90 AET, oC, max | n.s. | n.s. | 360
28. | Cold Soak Filtration Test, seconds, max | n.s. | n.s. | 360 200 (for use in temp below -12)

## Slide 19: Properties of biodiesel
Iodine value is specific to the feedstock
Higher its value affect the oxidative stability
Lower value result poor cold flow characteristics.

## Slide 20: Industrial Aspects
Storage stability
Stability has been achieved for biodiesel derived from palm oil
Requires synthetic antioxidants as additives to meet the stability properties, exception is palm based biodiesel

## Slide 21: Industrial Aspects
Total contaminants
The parameter is achievable after series of filtration
The reproducibility of the method is quite poor

## Slide 22: Storage Aspects
Biodiesel has good solvent property and may dissolve polymeric material on long term storage
Metallic container with exposed metals may act as catalysis for oxidation/hydrolysis and other unwanted reactions.
Tanks made up of aluminium, teflon or fluorinated polyethylene of polypropylene should be used
Outdoor tanks should be kept in cool shaded area

## Slide 23: Application Aspects
Practical concern has been observed by research for using biodiesel in existing diesel engine
Biodiesel having good solvency may dissolve the sediment caused by diesel and may lead to fuel filter clog
May require to replace filter initially when shifting diesel to biodiesel

## Slide 24: Application Aspects
Biodiesel has theoretically 10% less heating value compared to diesel fuel
Slightly low pulling power (2%) may be observed with biodiesel B20.

## Slide 25: Second generation biofuels
Lignocellulose derived ethanol
Green diesel by F-T process is superior to petro-diesel in many aspects
High cetane, zero sulfur and polyaromatics for green diesel

## Slide 26: Thank You